NMR relaxometry probes solvent-polarity-dependent molecular interactions in stimuli-responsive lyogels

Muhammad Adrian, *a Kathrin Marina Eckert,b,g M. Raquel Serial,a,c Artyom Tsanda,d,e Lukas Rennpferdt,f Stefan Benders,a,g Hoc Khiem Trieu,f Tobias Knopp,d,e Irina Smirnova,b,g Alexander Penna,g

a]	Institute of Process Imaging
Hamburg University of Technology

Denickestraße 17, 21073 Hamburg, Germany

b]	Institute of Thermal Separation Processes

Hamburg University of Technology

Eißendorferstraße 38, 21073 Hamburg, Germany

c]	Department of Process and Energy

Delft University of Technology

Leeghwaterstraat 39, 2628 CB Delft, The Netherlands

d]	Institute for Biomedical Imaging

Hamburg University of Technology

Am Schwarzenberg-Campus 3, 21073 Hamburg, Germany

e]	Section for Biomedical Imaging

University Medical Center Hamburg-Eppendorf

Lottestraße 55, 22529 Hamburg, Germany

f]	Institute of Microsystems Technology

Hamburg University of Technology

Eißendorferstraße 42, 21073 Hamburg, Germany

g]	United Nations University Hub on Engineering to Face Climate Change at the Hamburg University of Technology, United Nations University Institute of Water, Environment and Health, Hamburg, Germany

Table S1. List of used chemicals.

| Chemical | Purity | Supplier |
| --- | --- | --- |
| N-isopropylacrylamide (NIPAM) | > 98% | abcr |
| N,N′-methylenebis(acrylamide) (MBA) | > 99% | Sigma-Aldrich |
| Ammonium persulfate | > 98% | Sigma-Aldrich |
| Sodium metabisulfite | > 97% | Honeywell Fluka |
| Butyl acetate | ≥ 99.5% | Supelco |
| Ethanol | ≥ 99.9% | Chemsolute |

Table S2. Chemical structures of pNIPAM building blocks and organic solvents.

| Component | Chemical structure |  |
| --- | --- | --- |
| Monomer (N-(propan-2-yl)prop-2-enamide) |  |  |
| Ethanol |  |  |
| Butyl acetate |  |  |

Table S3. IDACs, hydrogen bond interaction energies, and Van der Waals interaction energies of NIPAM monomer in organic solvents at infinite dilution1.

| Organic Solvent | IDACs, ln(γᵢ∞) | Hydrogen bond interaction energies [kJ/mol] | Van der Waals interaction energies [kJ/mol] |
| --- | --- | --- | --- |
| Ethanol | 0.026 | -9.910 | -81.186 |
| Butyl acetate | 0.813 | -1.369 | -83.003 |

Table S4. Degree of swelling (Dos) of pNIPAM in ethanol and butyl acetate at equilibrium.

| Crosslinker concentration [g/g] | Ethanol2 - Dos [-] | Butyl acetate - Dos [-] |
| --- | --- | --- |
| 0.007 | 28.256 ± 2.076 | 3.032 ± 0.207 |
| 0.014 | 23.624 ± 5.059 | 2.308 ± 0.022 |
| 0.020 | 18.891 ± 1.955 | 2.106 ± 0.022 |
| 0.035 | 14.150 ± 1.003 | 1.943 ± 0.020 |
| 0.050 | 13.352 ± 2.591 | 1.959 ± 0.056 |

Table S5. Sample weight of pNIPAM in ethanol at equilibrium, as loaded onto the sample holder for NMR measurements.

| Crosslinker concentration [g/g] | Batch 1 - weight [mg] | Batch 2 - weight [mg] | Batch 3 - weight [mg] |
| --- | --- | --- | --- |
| 0.007 | 21 ± 1 | 14 ± 1 | 26 ± 1 |
| 0.014 | 21 ± 1 | 25 ± 1 | 20 ± 1 |
| 0.020 | 20 ± 1 | 17 ± 1 | 22 ± 1 |
| 0.035 | 17 ± 1 | 23 ± 1 | 17 ± 1 |
| 0.050 | 18 ± 1 | 15 ± 1 | 28 ± 1 |

Table S6. Sample weight of pNIPAM in butyl acetate at equilibrium, as loaded onto the sample holder for NMR measurements.

| Crosslinker concentration [g/g] | Batch 1 - weight [mg] | Batch 2 - weight [mg] | Batch 3 - weight [mg] |
| --- | --- | --- | --- |
| 0.007 | 20 ± 1 | 21 ± 1 | 23 ± 1 |
| 0.014 | 18 ± 1 | 19 ± 1 | 17 ± 1 |
| 0.020 | 17 ± 1 | 19 ± 1 | 17 ± 1 |
| 0.035 | 22 ± 1 | 25 ± 1 | 16 ± 1 |
| 0.050 | 15 ± 1 | 19 ± 1 | 17 ± 1 |

Table S7. T2 relaxation times and amplitude-normalized signal intensity of pNIPAM in ethanol at equilibrium.

| Crosslinker concentration [g/g] | Fraction | Ethanol - T2 [s] | Ethanol - Amplitude-normalized [-] |
| --- | --- | --- | --- |
| 0.007 | Bound solvent | 0.029 ± 0.002 | 0.009 ± 0.002 |
|  | Restricted solvent | 0.138 ± 0.021 | 0.013 ± 0.003 |
|  | Free solvent | 1.937 ± 0.112 | 1.000 ± 0.000 |
| 0.014 | Bound solvent | 0.032 ± 0.008 | 0.010 ± 0.004 |
|  | Restricted solvent | 0.146 ± 0.082 | 0.014 ± 0.010 |
|  | Free solvent | 1.873 ± 0.000 | 1.000 ± 0.000 |
| 0.020 | Bound solvent | 0.036 ± 0.002 | 0.015 ± 0.001 |
|  | Restricted solvent | 0.172 ± 0.010 | 0.013 ± 0.002 |
|  | Free solvent | 1.698 ± 0.000 | 1.000 ± 0.000 |
| 0.035 | Bound solvent | 0.035 ± 0.002 | 0.017 ± 0.004 |
|  | Restricted solvent | 0.192 ± 0.041 | 0.020 ± 0.011 |
|  | Free solvent | 1.645 ± 0.092 | 1.000 ± 0.000 |
| 0.050 | Bound solvent | 0.032 ± 0.002 | 0.016 ± 0.001 |
|  | Restricted solvent | 0.184 ± 0.011 | 0.014 ± 0.000 |
|  | Free solvent | 1.539 ± 0.000 | 1.000 ± 0.000 |

Table S8. T1/T2 ratios of pNIPAM in ethanol at equilibrium.

| Crosslinker concentration [g/g] | Fraction | Ethanol - T1/T2 [-] |
| --- | --- | --- |
| 0.007 | Bound solvent | 31.172 ± 6.604 |
|  | Restricted solvent | 9.415 ± 3.147 |
|  | Free solvent | 0.958 ± 0.073 |
| 0.014 | Bound solvent | 33.824 ± 4.565 |
|  | Restricted solvent | 11.678 ± 3.129 |
|  | Free solvent | 0.874 ± 0.000 |
| 0.020 | Bound solvent | 38.718 ± 5.227 |
|  | Restricted solvent | 11.949 ± 0.953 |
|  | Free solvent | 0.916 ± 0.073 |
| 0.035 | Bound solvent | 42.197 ± 3.216 |
|  | Restricted solvent | 12.057 ± 6.720 |
|  | Free solvent | 0.958 ± 0.073 |
| 0.050 | Bound solvent | 48.301 ± 3.678 |
|  | Restricted solvent | 12.858 ± 3.602 |
|  | Free solvent | 0.958 ± 0.073 |

Table S9. Self-diffusion coefficient (D) of pNIPAM in ethanol at equilibrium.

| Crosslinker concentration [g/g] | Ethanol - D [10-9 m2/s] |
| --- | --- |
| 0.007 | 0.947 ± 0.036 |
| 0.014 | 0.925 ± 0.005 |
| 0.020 | 0.855 ± 0.024 |
| 0.035 | 0.815 ± 0.016 |
| 0.050 | 0.797 ± 0.004 |

Table S10. T2 relaxation times and amplitude-normalized signal intensity of pNIPAM in butyl acetate at equilibrium.

| Crosslinker concentration [g/g] | Fraction | Butyl acetate - T2 [s] | Butyl acetate - Amplitude-normalized [-] |
| --- | --- | --- | --- |
| 0.007 | Bound solvent | 0.052 ± 0.007 | 0.058 ± 0.042 |
|  | Restricted solvent | 0.334 ± 0.049 | 1.000 ± 0.000 |
| 0.014 | Bound solvent | 0.027 ± 0.006 | 0.073 ± 0.038 |
|  | Restricted solvent | 0.192 ± 0.046 | 1.000 ± 0.000 |
| 0.020 | Bound solvent | 0.009 ± 0.005 | 0.029 ± 0.016 |
|  | Restricted solvent | 0.100 ± 0.018 | 1.000 ± 0.000 |
| 0.035 | Bound solvent | 0.006 ± 0.000 | 0.035 ± 0.011 |
|  | Restricted solvent | 0.059 ± 0.011 | 1.000 ± 0.000 |
| 0.050 | Bound solvent | 0.006 ± 0.000 | 0.036 ± 0.005 |
|  | Restricted solvent | 0.058 ± 0.004 | 1.000 ± 0.000 |

Table S11. T1/T2 ratios of pNIPAM in butyl acetate at equilibrium.

| Crosslinker concentration [g/g] | Fraction | Butyl acetate - T1/T2 [-] |
| --- | --- | --- |
| 0.007 | Bound solvent | 21.066 ± 4.386 |
|  | Restricted solvent | 2.977 ± 0.303 |
| 0.014 | Bound solvent | 26.952 ± 8.564 |
|  | Restricted solvent | 4.283 ± 1.158 |
| 0.020 | Bound solvent | 34.902 ± 3.356 |
|  | Restricted solvent | 6.266 ± 0.603 |
| 0.035 | Bound solvent | 55.695 ± 10.351 |
|  | Restricted solvent | 10.489 ± 1.009 |
| 0.050 | Bound solvent | 69.418 ± 6.709 |
|  | Restricted solvent | 11.072 ± 0.000 |

Table S12. Self-diffusion coefficient (D) of pNIPAM in butyl acetate at equilibrium.

| Crosslinker concentration [g/g] | Butyl acetate - D [10-9 m2/s] |
| --- | --- |
| 0.007 | 0.577 ± 0.078 |
| 0.014 | 0.404 ± 0.070 |
| 0.020 | 0.326 ± 0.029 |
| 0.035 | 0.243 ± 0.043 |
| 0.050 | 0.290 ± 0.018 |

Table S13. Self-diffusion coefficient (D) of bulk ethanol and butyl acetate.

| Component | D [10-9 m2/s] |
| --- | --- |
| Ethanol | 1.106 ± 0.005 |
| Butyl acetate | 1.621 ± 0.004 |

Table S14. Solvent exchange rates (kex) between free and bound solvent of pNIPAM in ethanol at equilibrium.

| Crosslinker concentration [g/g] | Ethanol - kex [1/s] |
| --- | --- |
| 0.007 | 34.582 ± 1.826 |
| 0.014 | 31.825 ± 6.278 |
| 0.020 | 28.581 ± 1.477 |
| 0.035 | 29.530 ± 1.607 |
| 0.050 | 31.530 ± 1.631 |

Table S15. Solvent exchange rates (kex) between restricted and bound solvent of pNIPAM in butyl acetate at equilibrium.

| Crosslinker concentration [g/g] | Butyl acetate - kex [1/s] |
| --- | --- |
| 0.007 | 22.269 ± 2.660 |
| 0.014 | 41.895 ± 7.485 |
| 0.020 | 117.329 ± 39.773 |
| 0.035 | 189.356 ± 14.206 |
| 0.050 | 189.527 ± 12.640 |

Table S16. Standard Gibbs energy of binding (ΔBG°) between free and bound solvent of pNIPAM in ethanol at equilibrium.

| Crosslinker concentration [g/g] | Ethanol - ΔBG° [kJ/mol] |
| --- | --- |
| 0.007 | 11.079 ± 0.417 |
| 0.014 | 10.396 ± 0.895 |
| 0.020 | 9.990 ± 0.196 |
| 0.035 | 9.433 ± 0.526 |
| 0.050 | 9.903 ± 0.179 |

Table S17. Standard Gibbs energy of binding (ΔBG°) between restricted and bound solvent of pNIPAM in butyl acetate at equilibrium.

| Crosslinker concentration [g/g] | Butyl acetate - ΔBG° [kJ/mol] |
| --- | --- |
| 0.007 | 6.935 ± 1.322 |
| 0.014 | 6.369 ± 1.009 |
| 0.020 | 8.602 ± 1.080 |
| 0.035 | 8.180 ± 0.682 |
| 0.050 | 8.093 ± 0.338 |

Figure S1. NMR glass sample holder CAD design.

Figure S2. L-curve Tikhonov regularization parameter (alpha = 0.1) for lyogel in EtOH and BuAc with varied crosslinker concentration (0.007 – 0.050 g/g).

References

[1] Eckert KM, Müller S, Luinstra GA, Smirnova I. Exploring pNIPAM lyogels: Experimental study on swelling equilibria in various organic solvents and mixtures, supported by COSMO-RS analysis. Fluid Phase Equilibria. 2024 Nov 1;586:114182.

[2] Eckert KM, Bonsen J, Hajnal A, Gmeiner J, Hasse J, Adrian M, Karsten J, Kißling PA, Penn A, Fiedler B, Luinstra GA. Enhancing swelling kinetics of pNIPAM lyogels: The role of crosslinking, copolymerization, and solvent. Fluid Phase Equilibria. 2025 May 6:114462.