# §250113-Experimental-Plan-Coating-Layer

Metadata

Topic:: Experiment for coating layer impedance of multi layer coatings with sodium benzoate
Context:: SFB1615 A07
Devices:: {Zurich Impedance Analyzer,Profilometer}

# Target

Generate thicker layers of sodium benzoate on top of the PCB electrodes than the previous ones in the range of  .

# Materials

- Zurich Impedance Analyzer

  - -

  - Impedance range = auto

  - Voltage and current range = auto

- Profiometer

  - Focus on the electrode position not the whole layer

- PCBs

  - Conductive

  - Printed in Freiburg

  - Capacitive

- Others

  - Pipette

  - sodium benzoate solution

# Procedure

- Droplets of  sodium benzoate solution on top of the pcb electrodes

  - Spread the solution to form a thin uniform layer

- Dry in oven at  until it is dry

  - dry is defined as the state, where the electrical impedance has a phase angle of

  - Not to be mistaken with a "lift-off" of a layer from the electrodes -> visual scan

- Measure the dried layer

  - Perform impedance sweep

  - Measure the layer thickness

- Add another layer and repeat the drying procedure

- At some point stop adding layers (HOW MANY LAYERS?)

  - Measure impedance and layer thickness

# File names

e.g.

| FileName (string) | layer_thickness in mm (double) | coating_no_lift-off (bool) |
| --- | --- | --- |
| C_Ca_V1_N0_1.txt | 0.23 | 1 |
| C_Ca_V1_N0_1.txt | 0.31 | 1 |

## Keys

- C

  - Circular electrode

- Ca / Co

  - Capacitive or Conductive electrode

- V1 / V2

  - Geometry version (big or small)

- N0 / N1 / N2

  - Of each geometry, there are up to 3 copies

- i = 1,2,3,...

  - number of layers