Supporting Information belonging to

Iron(III) Ion reinforced P(NiPAAm-co-AA) Beads as tunable Smart Organogels

Johannes Gmeiner, Jonah Hasse, Gerrit A. Luinstra*

Institute of Technical and Macromolecular Chemistry, University of Hamburg,

Bundesstrasse 45, 20146 Hamburg, Germany

E-Mail: luinstra@chemie.uni-hamburg.de (G.A.L.)

Table S1. Absorption maximum determined from the UV-Vis spectra before and after Fe uptake

|  | Absorbance t=0 (Start) | Absorbance t=48h (End) | Δ Absorbance (Start - End) |  |
| --- | --- | --- | --- | --- |
| Fe-Low | 0.57002 | -0.00743 | 0.57745 |  |
| Fe-Med | 1.855 | 0.78744 | 1.06756 |  |
| Fe-High | 0.92787 | 0.66734 | 0.26053 |  |

Table S2. Initial weights and results of the elemental analysis of Fe

| ZEA ID | Sample weight | Sample weight | measured Fe | Fe | Fe |
| --- | --- | --- | --- | --- | --- |
|  | mg/15 mL | mg/L | mg/L | mg/g | % |
| Fe-Low | 17.14 | 1142.67 | 38.6797 | 33.850 | 3.39 |
| Fe-Med | 14.02 | 934.67 | 63.7286 | 68.183 | 6.82 |
| Fe-High | 18.21 | 1214.00 | 103.8186 | 85.518 | 8.55 |

- b)

c)

Figure S1. UV-Vis spectra of Fe solutions before and after Fe uptake of a) Fe-Low, b) Fe-Mid, c) Fe-High

Figure S2. UV-Vis spectrum of KSCN solutions for calibration of Fe(III)ion concentration in ethanolic solution  b) Calibration line to determine the TEMPO absorbance of the organogels

a)						b)

Figure S3. Time constant τ1 from an exponential fit a) of the shrinking process of the organogels over 30 min in  neat EtOAc and b) of the swelling process over 30 min in neat EtOH. The curves shown are from cycle 5 and the given values are the mean of all 6 cycles.

Figure S4. Cyclic exposure for 30 min of OG10-10 beads to ethanol and ethyl acetate (green underlay), showing intermediate shrinkage in the swelling after placement in ethanol (from ethyl acetate).