## Slide 1
Sustainable Lignin Polymer Foaming Using High Pressure Carbon Dioxide
Razan Altarabeen, Christin Zimmer, Carsten Zetzl, Irina Smirnova
Institut für Thermische Verfahrenstechnik, Technische Universität Hamburg
Jahrestreffen der ProcessNet-Fachgruppe Hochdruckverfahrenstechnik (HDVT), 2021

## Slide 2
Porous Lignous Organic Materials

## Slide 3
Biorefinery

## Slide 4
Increase demand of polymeric foams
Target properties
Lignin polylactide (PLA) foams
Sustainable resources
Objective

## Slide 5
Introduction: lignin as nucleation agent
Provides nucleation sites
Improves crystallization kinetics
Biodegradable
Enhances flame retardancy
https://polymer-additives.specialchem.com/centers/polypropylene-nucleation-center/how-do-nucleating-agents-work

## Slide 6
Solid state foaming:
e.g. Thermally induced process using pentane
Melt state foaming:
e.g. Addition of blowing agent during extrusion
Introduction: conventional process

## Slide 7
Every additive plays an important role into building the final foam structure
Introduction: conventional process
Nucleation agent
Cellular structure
Blowing agent
Foaming
Porosity
density
Filler
Stability
Particle size
Melting point
Polymeric Matrix

## Slide 8
Blowing agents
Blowing agent
Chemical blowing agent
e.g. Sodium bicarbonate
Physical blowing agent
e.g. chlorofluorocarbons (CFCs) & hydrochlorofluorocarbons (HCFCs)
No good control of the porosity
presence of residues
Greenhouse gases
CO2 as an environment-friendly alternative?

## Slide 9
CO2 as a blowing agent
Introduction of a thermodynamic instability
Nucleation of cells
Saturation of CO2
high pressures
Super-saturation reducing the pressure or increasing the temperature.
Good solubility in polymer blends
Acts as a plasticizer
Lowers viscosity and glass transition temperature
Controls pore generation and growth

## Slide 10
Experimental Plan
Extrusion
Lignin characterization
Compounding and extrusion
Foaming behavior
Batch CO2 foaming
Other blowing agents foaming
Continuous foaming
Extrusion coupled with CO2 foaming
Characterization tests

## Slide 11
Materials
Name | Extraction Method | Klason content | Particle size (d90/µm) | Moleculer weight (kDa) | Mositure content (wt%)
Hydrolytic 1 | Novel Biorefinery | 68.2% | 72.4 | 8.0 | 1.9
Hydrolytic 2 |  | 78.9% | 38.6 | 13.3 | 4.8
Supercritical water |  | 80.8% | 36.2 | 60.1 | 0.6
Lignosulfonate | Sulfite pulping | - | 159.2 | - | 5.6
Soda | Soda pulping | 95% | 89.6 | 9.2 | 5.2

## Slide 12
First step: Compounding and Extrusion
Methodology
Twin screw extruder
T = 170 °C
rpm= 180 U/min
Lignin PLA foams with 10, 20 and 30 wt% lignin

## Slide 13
Second step: Batch CO2 Foaming
Methodology
Retention time: 120 minutes
Depressurization time (seconds): 60 ± 5
Pressure (bar): 60
Temperature (°C): 60

## Slide 14
, tdep,1 = 60 s, tdep,3 = 74 s, tdep,3 = 152 s
Second step: Batch CO2 Foaming
Short depressurization time  Homogenous cellular structure
Long depressurization time  cell coalescence
Results
Depressurization time (seconds): t1 = 60 , t2 = 74 , t3 = 152

## Slide 15
Results: Volume expansion ratio
Chart: Lignin Type
| 10H1 | 20H1 | 30H1 | 10H2 | 20H2 | 30H2 | 10SW | 20SW | 30SW | 10L | 20L | 30L | 10S | 20S | 30S
VER | 8.3635 | 4.3503 | 4.9898 | 3.2239 | 4.8326 | 6.2146 | 5.4291 | 7.7152 | 13.4276 | 6.3909 | 7.8829 | 3.3803 | 8.018 | 8.8009 | 3.6206
10: 10 wt% lignin in PLA foam
20: 20 wt% lignin in PLA foam
30: 30 wt% lignin in PLA foam
The change of the foam VER varies with lignin type.
Hydrolytic 1
Hydrolytic 2
Notes: E: Lower Tg C: 70.49
F: high thermal Stability Tg
F: D90 29,8 but higher glass transition temp – higher thermal stability

## Slide 16
Results: Volume expansion ratio
Hydrolytic 1 lignin with:
(1) 10, and (2) 30 wt%.
Molecular weight: 8.0 (kDa)
Supercritical water lignin with:
(1) 10 and (2) 30 wt %.
Molecular weight: 60.1 (kDa)
1
2
2
1
Influence of molecular weight (thermal stability) on melt strength is more pronounced at higher lignin concentration.
Higher molecular weight  Higher melt strength  More stable cellular structure

## Slide 17
Results: Cellular Structure
Hydrolytic 1: moisture 1.9 wt%
Hydrolytic 2: moisture 4.8 wt%
Lignin PLA foams with the same lignin concentration 20 wt%
Higher moisture content  Heterogeneous cellular structure

## Slide 18
Chart: Lignin Type
| 10H1 | 20H1 | 30H1 | 10H2 | 20H2 | 30H2 | 10SW | 20SW | 30SW | 10L | 20L | 30L | 10S | 20S
VER | 0.20068 | 0.13153 | 0.1616 | 0.15375 | 0.11402 | 0.38192 | 0.19413 | 0.1764 | 0.13438 | 0.21765 | 0.1506 | 0.25973 | 0.18102 | 0.17765
Results: Density
The Lignin PLA foams had an average densities of 0.19 g/cm³.
Higher klason content  lower density
Rarrange in respect to klason content
H1
H2
S
SW
L
Hydrolytic 1
Hydrolytic 2
Supercritical
water
Lignosulfonate
Soda
10: 10 wt% lignin in PLA foam
20: 20 wt% lignin in PLA foam
30: 30 wt% lignin in PLA foam

## Slide 19
Results: Flammability
lignin can be considered a bio-flame retardant owning to its char formation of 35-40% *
during combustion.
The formed charred layers protect the underlying materials from rephrase
the transferred heat and flame and act as a physical barrier.
Sample | Flame spread speed (mm/min)
Pure PLA | 17.4
10% hydrolytic 1 lignin | 12 .0
30% hydrolytic 1 lignin | 3.6
Charring behavior of 30 wt % lignin
PLA foams

## Slide 20
Results: Cellular Structure
Lignin provides better foaming in comparison with wood fibers *.

## Slide 21
Outlook: Extrusion process assisted by carbon dioxide

## Slide 22
Key Parameters:
Nucleation mechanism
Lower gibbs energy  higher nucleation:
gibbs energy changed with CO2
(lower than solubility limit, Homogenous nucleation)
gibbs energy changed with Lignin
Addition of term to describe nucleation by lignin
(Heterogeneous nucleation)

## Slide 23
Key Parameters:
Solubility of CO2
Solubility
Interfacial tension
Nucleation rate
Finer pore structure

## Slide 24
Key Parameters
Glass transition temperature (Tg)
Faster pressure drop  faster increase in Tg
Increase in high molecular weight lignin  faster increase in Tg
Extrudates oven dried at 70 ◦C; (a) control, (b) 7% whey protein concentrate
a
b
Analogy to use of lignin as stabilizing agent to enhance Tg

## Slide 25
Next steps
Understanding nucleation mechanism in continuous CO2 foaming
Influence of lignin percentages on Tg (or critical temp)
Solubility of CO2 in lignin/polymer blends
Describing the heterogeneous nucleation rate

## Slide 26
References
[1] R. Auras, B. Harte, and S. Selke, “An Overview of Polylactides as Packaging Materials,” Macromol. Biosci., vol. 4, no. 9, pp. 835–864, Sep. 2004, doi: 10.1002/mabi.200400043.
[2] Q. Zong, A. Xu, K. Chai, Y. Zhang, and Y. Song, “Increased expansion ratio, cell density, and compression strength of microcellular poly(lactic acid) foams via lignin graft poly(lactic acid) as a biobased nucleating agent,” Polym. Adv. Technol., p. pat.4944, Jun. 2020, doi: 10.1002/pat.4944.
[3] W. Yang et al., “Synergic effect of cellulose and lignin nanostructures in PLA based systems for food antibacterial packaging,” Eur. Polym. J., vol. 79, pp. 1–12, Jun. 2016, doi: 10.1016/j.eurpolymj.2016.04.003.
[4] M. Sauceau, J. Fages, A. Common, C. Nikitine, and E. Rodier, “New challenges in polymer foaming: A review of extrusion processes assisted by supercritical carbon dioxide,” Prog. Polym. Sci., vol. 36, no. 6, pp. 749–766, Jun. 2011, doi: 10.1016/j.progpolymsci.2010.12.004.
[5] D. L. Tomasko et al., “Development of CO2 for polymer foam applications,” J. Supercrit. Fluids, vol. 47, no. 3, pp. 493–499, Jan. 2009, doi: 10.1016/j.supflu.2008.10.018.
[6] H. Ruckdäschel, V. Altstädt, and A. H. E. Müller, “Foaming of Polymer Blends – Chance and Challenge,” Cell. Polym., vol. 26, no. 6, p. 14, 2007.

## Slide 27
Thank you for your attention